Biorefining in Electrochemical Reactors: Conversion of Biomass-Derived Compounds to Various Platform Chemicals

Suddhasatwa Basu
FIPI Chair Professor, Indian Institute of Technology Delhi

At present, Visiting Professor, Washington University in St Louis, MO (Fulbright Academic & Professional Excellence Fellow) e-mail: sbasu@iitd.ac.in

EVENTS

June 9		11 am – 12:30 pm	Seminar in AME 106 (2003 Levy Ave)

June 10		9 am – 6 pm		Individual Meetings* with Dr. Basu

June 11		9 am – 12 pm		Individual Meetings* with Dr. Basu

1:30 – 2:30 pm		Fulbright Roundtable Discussion in 
 				Beth Moore Lounge, Longmire (FSU)

*Sign up for an individual meeting with Dr. Basu in Engineering B-202 here

Prof. Suddhasatwa Basu holds Federation of Indian Petroleum Industry (FIPI) Chair Professor on Clean Energy at IIT Delhi. At present he is visiting Professor in Energy, Environment & Chemical Engineering Department of Washington University in St Louis as a Fulbright Academic & Professional Excellence Fellow. He was the Director of CSIR-Institute of Minerals & Materials Technology, Bhubaneswar, India and the Director of Central Institute Mining & Fuel Research, Dhanbad, India. He has vast work experience on development of materials for energy conversion and storage devices – Green H2 & Fuel Cells technologies and rechargeable battery materials, electro-synthesis, wastes to wealth technologies for circular economy. He has published more than 300+ articles in high impact journals with H-index 57, 10 patents and 2 technologies transferred. He is a Fellow of Indian National Science Academy, National Academy of Science of India, Indian National Academy of Engineering, Royal Society of Chemistry UK and received Herdillia Award, Dr A. V. Rama Rao Foundation's Research Award, SMC Gold Medal, MRSI Medal. He is Editor/Assoc Editor/Ed Board member of several international journals published by Wiley, IOP Science, Springer-Nature, Oxford University Press and Am Chemical Soc.

ABSTRACT  The bio-electro-refinery refers to the bio-refinery integrated with the electrochemical and photo-electrochemical conversion of intermediate biomass-derived compounds to value-added chemicals.1,2 The thermochemical treatment of paddy stubble was done using fast pyrolysis obtained a mixture of organic compounds, termed as bio-oil. Bio-oil comprises organics such as phenol, catechol, p-cresol, furfural (FF), acetic acid, 2-methoxyphenol, and hydroquinone.3 As a component of bio-electro-refinery, the electrocatalytic conversion of biomass-derived FF provides platform chemicals such as furfuryl alcohol (FA), hydrofuroin and furoic acid (FU) used in pharmaceuticals, and bio-fuel industries. The electrocatalytic hydrogenation (ECH) of FF was dependent upon the availability of adsorbed hydrogen and FF, type of electrocatalyst and applied potential. Cu-NPNi/NF was developed through the etching of Cu from a co-electrodeposited Ni-Cu electrode on a Ni-foam substrate followed by a re-electrodeposition of Cu. Cu-NPNi/NF exhibited a porous, and bimetallic form of Ni-Cu, which yielded a high FA (118.7 ± 8 μmol h−1 cm−2) and HF (176.3 ± 3.4 μmol h−1 cm−2) generation rates determined at −1.45 V vs. Ag/AgCl/sat KCl after 1 h of electrolysis in an alkaline electrolyte. 100% conversion of furfural was observed after 2 h of electrolysis with the same catalyst. The high rate of FA and HF formation was ascribed to enhanced adsorbed FF because of the formation of Cu-nanoplates and bimetallic Ni–Cu.4 The utilization of solar energy was further utilized to reduce the electrical energy requirement in the photoelectrochemical conversion of FF. Herein, the FF ECH was paired with photoelectrochemical oxidation of FF to generate FA at cathode and FU at non-noble TiO2 photoanode in a batch photoelectrochemical cell. A 50% electrical energy saving efficiency was obtained due to the use of solar illumination. To further increase the cell capacity (5 times) and overcome mass transfer limitations, a flow photoelectrochemical cell was employed yielding an increase in FA and FU generation rates.5-7 I shall further discuss electrochemical conversion of biomass based HMF (5-(Hydroxymethyl) furan-2-carbaldehyde) into FDCA (2, 5-Furandicarboxylic acid) and hydrogen gas simultaneously. The conversion process occurs within a 3D-printed flow electrolyzer operating under alkaline conditions (pH 13) at room temperature and pressure. At room temperature and pressure, a single pass through an electrochemical cell, yields 287.5 µmol/h of FDCA, an industrially significant precursor of bioplastic. Upto 80 % conversion of HMF is seen at flowrate of 0.5 ml/min in a single pass. These results are achieved with a potential bias of 3.5 V. This technological advancement in electrochemical flow reactors facilitates the uninterrupted production of value-added chemicals and fuels from biomass derived chemicals under ambient environment8,9.

References

1. Moncada, J.; Tamayo, J. A.; Cardona, C. A. Integrating First, Second, and Third Generation Biorefineries: Incorporating Microalgae into the Sugarcane Biorefinery. Chem. Eng. Sci. 2014, 118, 126–140. https://doi.org/10.1016/j.ces.2014.07.035.

2. Siwal, S. S.; Zhang, Q.; Saini, A. K.; Gupta, V. K.; Roberts, D.; Saini, V.; Coulon, F.; Pareek, B.; Thakur, V. K. Recent Advances in Bio-Electrochemical System Analysis in Biorefineries. J. Environ. Chem. Eng. 2021, 9, 105982. https://doi.org/10.1016/j.jece.2021.105982.

3. Wang, Y.; Zeng, Z.; Tian, X.; Dai, L.; Jiang, L.; Zhang, S.; Wu, Q.; Wena, P.; Fua, G.; Liua, Y.; et al. Production of Bio-Oil from Agricultural Waste by Using a Continuous Fast Microwave Pyrolysis System. Bioresour. Technol. 2018, 269, 162–168. https://doi.org/10.1016/j.biortech.2018.08.067.

4. Dixit, R. J.; Bhattacharyya, K.; Ramani, V. K.; Basu, Suddhasatwa, Electrocatalytic Hydrogenation of Furfural Using Non-Noble-Metal Electrocatalysts in Alkaline Medium. Green Chem. 2021, 23, 4201–4212. https://doi.org/10.1039/d1gc00579k.

5. Dixit, R. J.; Singh, A.; Ramani, V. K.; Basu, Suddhasatwa, Electrocatalytic Hydrogenation of Furfural Paired with Photoelectrochemical Oxidation of Water and Furfural in Batch and Flow Cells. React. Chem. Eng. 2021, 6 (12), 2342–2353. https://doi.org/10.1039/d1re00080b.

6. Biswajit S De, Ram Ji Dixit, Abhas Anand, Suddhasatwa Basu, Experimental, Equilibrium Modelling, and Column Design for the Reactive Separation of Biomass-Derived 2-Furoic Acid, Can J Chem Eng. 2023, 101, 3167–3179 https://doi.org/10.1002/cjce.24823

7. Ram Ji Dixit, Photo and electrochemical chemical conversion of biofuel, Ph.D. (2023)

8. Aditya Singh, Karan Singh, Ram Ji Dixit, Biswajit Samir De, Suddhasatwa Basu, Co-generation of hydrogen and FDCA from biomass-based HMF in 3D-printed flow electrolyzer, Ind Eng Chem Res, 2024, 63(49), 21180−21189 https://doi.org/10.1021/acs.iecr.4c01213

9. Muthuraja Velpandian, Kiruthieek Paranitharan, Suddhasatwa Basu, Vanadium Doped Cobalt Based Metal Organic Framework For Enhanced FDCA Electrosynthesis: Effect of Doping, ChemNanoMat, 2026 12(3), e202500599 http://dx.doi.org/10.1002/cnma.202500599